FASTSET™ CONCRETE MIX

A rapid hardening concrete mix designed with a 20-30 minute set time, allowing for mixing, pouring and finishing. Use at any thickness from 1-1/2” to 24”.

Use to build or repair:

• Street repairs

• Concrete parking lots

• Highways

• Concrete floors

• Bridge decks

• Sidewalks

Compressive Strength ASTM C39

3 Hours	3000 psi	20.7 MPa

24 Hours	5000 psi	34.5 MPa

7 Days	6000 psi	41.3 MPa

28 Days	7000 psi	48.3 MPa

Exceeds the requirements of ASTM C 928 R-3