FASTSET™ NON-SHRINK GROUT

For structural concrete repairs from ¼” to 24” deep.  30 minute set time, non shrink characteristics & rapid strength gain.  Can be mixed to a plastic, flowable or fluid consistency.

Use for anchoring & grouting:

• Anchor bolts

• Steel column bases

• Bearing plates

• Floor leveling

• Pre-cast concrete keyways

Compressive Strength ASTM C109

Time		Fluid			Flowable			Plastic

3 Hours		2000 psi (13.8 MPa)	2500 psi (17.2 MPa)	3000 psi (20.7 MPa)

24 Hours		4000 psi (27.6 MPa)	4500 psi (31.0 MPa)	5000 psi (34.5 MPa)

7 Days		5000 psi (34.5 MPa)	5500 psi (37.9 MPa)	6000 psi (41.3 MPa)

28 Days		6500 psi (44.8 MPa)	7500 psi (51.7 MPa)	8000 psi (55.1 MPa)

Exceeds ASTM C 928 R-3 and ASTM C 1107.