FASTSET™ REPAIR MORTAR

A low-sag repair mortar formula. Ideal for vertical & overhead repairs. 20-30 minute working time & unique properties allow sculpting of the material during placement.

Use for repairing:

• Pre-stress panels

• Retaining walls

• Tunnels

• Loading docks

• Bridge columns

• Curbs/steps

Compressive Strength ASTM C109 Modified

3 Hours	2000 psi	13.8 MPa

24 Hours	4000 psi	27.6 MPa

7 Days	5000 psi	34.5 MPa

28 Days	6000 psi	41.4 MPa

Exceeds the requirements of ASTM C 928 R-2