FASTSET™ DOT MIX & FASTSET™ DOT MIX - EXTENDED

For structural concrete repair of bridge decks, roadways & parking decks from ½” to 24” thick.  Can be extended with up to 25 lb. of 3/8” stone or gravel with a top size of up to ½” for patched over 2” thick.  Also available in pre-extended formulas (No. 1244-80).

Use for anchoring & grouting:

• Structural concrete repair

• Bridge decks

• Roadways

• Parking deck applications

Compressive Strength ASTM C109

1½ Hours	3000 psi	20.7 MPa

3  Hours	4500 psi	31.0 MPa

24 Hours	6500 psi	44.8 MPa

7 Days	8000 psi	55.1 MPa

28 Days	10,000 psi	69.0 MPa

Exceeds the requirements of ASTM C 928 R-3

Exceeds DOT region 3 requirements for exposure to de-icing chemicals