NON-SHRINK GENERAL PURPOSE GROUT

High strength, non-metallic portland cement based grout including expansive additives. Can be mixed to a plastic, flowable or fluid consistency.

Use For:

• Grouting, anchoring and general construction applications

Compressive Strength at 28 Days

Plastic	10,000 psi	68.9 MPa

Flowable	9,000 psi	62.1 MPa

Fluid	8,000 psi	55.2 MPa

Complies with ASTM C 1107 and Army Corp of Engineers CRD 621