PORTLAND CEMENT – No. 1124

Can be mixed with aggregate and other ingredients to make concrete mix, mortar mix and base coat stucco.

Available in Type I, Type 1/II, Type II and Type III.

To make Concrete Mix:

• 3 Parts Gravel

• 2 Parts All-Purpose Sand

• 1 Part Portland Cement (by volume)

To make Type S Mortar Mix:

• 3½ to 4½ Parts Masonry Sand

• ½ Part Hydrated Lime

• 1 Part Portland Cement (by volume)

Complies with current ASTM C 150 and Federal Specifications for portland cement.