RAPID ROAD REPAIR & RAPID ROAD REPAIR - EXTENDED

Fast-setting, rapid-hardening structural repair mortar, designed to make pavement repairs to concrete pavement.  Alkali-resistant fiber reinforced for improved flexural performance.  Available in pre-extended formula (No. 1242.80)

Use For Repairing:

• Highways

• Bridge decks

• Runways

• Concrete footings

• Parking garages	• Driveways

Exceeds: 3000 psi (20.7 MPa) at 1 hour

8300 psi (57.5 MPa) at 28 days

Exceeds ASTM C 928 R-3